Quality and Reliability Data

Last Updated on 7/10/2002

### Atmel Serial EEPROM AT24C08A

Description		8K 2-Wire Shrink w/ Full WP

Entry Date		11/27/01

Tapeout Date		2/25/02

Fab Out Date		5/3/02

Char Date		6/6/02

Release Engineer	Matt Rocco

Sustaining Engineer	Matt Rocco

#### Package Options

| PACKAGE_OPTION |  | FIT/ROUTE |  | WAIVER |  | COMMENTS |
| --- | --- | --- | --- | --- | --- | --- |
| EIAJ 8LD |  | YES |  | NO |  |  |
| PDIP 8LD |  | YES |  | NO |  |  |
| SOIC 8LD |  | YES |  | NO |  |  |
| TSSOP 14LD |  | YES |  | NO |  |  |
| DBGA |  | NO |  | NO |  |  |
| LAP 5X6 |  | YES |  | NO |  |  |
| LAP 5X8 |  | YES |  | NO |  |  |
| TSSOP |  | YES |  | NO |  |  |

##### Voltage Options

|  | AUTOMOTIVE | INDUSTRIAL | COMMERCIAL |
| --- | --- | --- | --- |
| VOLTAGE | GRADE | GRADE | GRADE |
| 5.00 | PENDING | YES | YES |
| 2.70 | PENDING | YES | YES |
| 1.80 | PENDING | YES | YES |

Write Endurance

| TRACK # | DATE | TEST_POINT | FAIL_QTY | COMMENTS |
| --- | --- | --- | --- | --- |
| 8426 |  | 1000000 | 0 | NO FAILS |

##### Life Test

| TRACK # | DATE | TEST_POINT | FAIL_QTY | COMMENTS |
| --- | --- | --- | --- | --- |
| 8426 |  | 504 | 0 | NO FAILS |

Data Retention

| TRACK # | DATE | RD_POINT | FAIL_QTY | COMMENTS |
| --- | --- | --- | --- | --- |
| 8426 |  | 504 | 0 | NO FAILS |

# PRODUCT QUALIFICATION POLICY

Die Fabrication Process

- Each Microcircuit Group Is Qualified Every 52 Weeks.

- Microcircuit Groups Are Defined Per Mil-PRF-38535 & JEDEC 26.

- The Most Complex Product Available Is Used For Qualification.

- Only Qualified Product May Be Shipped.

Package Assembly Process

- Each Package Family Is Qualified Every 36 Weeks.

- Each Assembly Subcontractor Is Qualified Every 36 Weeks.

- Package Families Are Defined Per MIL-PRF-38535 & JEDEC 26.

- The Worst Case Package Is Used For Qualification.

- Only Qualified Product May Be Shipped.

# DIE FABRICATION PROCESS QUALIFICATION

# Test Flow & Conditions

Baseline Electrical Parameters Per Device Specification

- Dynamic Lifetest Per MS883, M1005 - 77 Dev, Acc on 1 Failure.

1000 Hours @ 1250C or 500 Hours @1500C.

- Data Retention Bake (NVM Only) - 77/1.

1000 Hours @ 1500C or 500 Hours @ 2500C.

- Write Endurance (NVM Only, All Product) - 100/1.

100,000 Cycles @ 250C.

- Latchup (All Product) Per JEDEC 17 - 6/0.

150 mA Trigger Current At Maximum Operating Temperature.

- ESD Sensitivity (All Product) Per MS883, M3015.

Human Body Model (15000, 100pf). 500V, 1KV, 2KV, 3KV, 4KV.  5 total/ 1 at each voltage

# PACKAGE ASSEMBLY PROCESS QUALIFICATION

Plastic - Test Flow & Conditions - Environmental

### Baseline Electrical Parameters Per Device Specification

- Static Biased Lifetest Per JS22, MA101 - 77 Dev, Acc on 1 Fail.

1000 Hours @ 85% Relative Humidity & 850C.

- Data Retention Bake (NVM Only) - 100/1.

1000 Hours @ 1500C.

- Autoclave Per JS22, MA102 - 77/1.

96 Hours @ 100% Relative Humidity & 2 Atm.

- Resistance to Soldering Heat Per JS22, MB106 - 22/0.

2600C Solder Dip.

- Temperature Cycle Per MS883, M1010 - 77/1.

1000 Cycles, -650C to 1500C.

# PACKAGE ASSEMBLY PROCESS QUALIFICATION

Test Flow & Conditions - Mechanical

### Physical Dimensions Per MS883, M2016.  15/0

- Lead Integrity Per MS883, M2004.  45/0

- Adhesion of Lead Finish Per MS883, M2025.  15/0

- Resistance To Solvents Per JS22, MB107 or MS883, M2015.  3/0

- Solderability Per MS883, M2003.  38/1 8 Hours Steam Age. 2600C Solder Dip Lead Free Package.  2450C For Regular Plastic Packages.

Characterization Data

Characterization Program

CH24C08  Serial EEPROM  11-03-98

----------------------------------------

Opens:

Shorts:

Lkg @5.5V, #1 =  00.03      UA

Lkg @5.5V, #2 =  00.04      UA

Lkg @5.5V, #3 =  00.03      UA

Lkg @5.5V, #5 =  00.08      UA

Lkg @5.5V, #6 =  00.03      UA

Lkg @5.5V, #7 =  00.30      UA

ISB @ 06.000  VOLTS =  003.7      UA

ISB @ 05.500  VOLTS =  002.9      UA

ISB @ 05.000  VOLTS =  002.3      UA

ISB @ 04.500  VOLTS =  001.8      UA

ISB @ 04.000  VOLTS =  001.4      UA

ISB @ 03.500  VOLTS =  001.1      UA

ISB @ 03.000  VOLTS =  000.8      UA

ISB @ 02.500  VOLTS =  000.5      UA

ISB @ 02.000  VOLTS =  000.3      UA

ISB @ 01.500  VOLTS =  000.2      UA

Ack & Slaves:

Ack LVcc = 01.200  VOLTS limit!

WR-RD byte LVcc = 01.420  VOLTS

WR-RD array LVcc = 01.580  VOLTS

WR/RD MATRIX AT 100KHz:

5.5v 5.0v 4.5v 3.6v 2.7v 2.5v 1.8v 1.7v

---- ---- ---- ---- ---- ---- ---- ----

wrCHK @5.5v, rd:  P    P    P    P    P    P    P    P

wrICK @5.5v, rd:  P    P    P    P    P    P    P    P

wrCHK @5.0v, rd:  P    P    P    P    P    P    P    P

wrICK @5.0v, rd:  P    P    P    P    P    P    P    P

wrCHK @4.5v, rd:  P    P    P    P    P    P    P    P

wrICK @4.5v, rd:  P    P    P    P    P    P    P    P

wrCHK @3.6v, rd:  P    P    P    P    P    P    P    P

wrICK @3.6v, rd:  P    P    P    P    P    P    P    P

wrCHK @2.7v, rd:  P    P    P    P    P    P    P    P

wrICK @2.7v, rd:  P    P    P    P    P    P    P    P

wrCHK @2.5v, rd:  P    P    P    P    P    P    P    P

wrICK @2.5v, rd:  P    P    P    P    P    P    P    P

wrCHK @1.8v, rd:  P    P    P    P    P    P    P    P

wrICK @1.8v, rd:  P    P    P    P    P    P    P    P

wrCHK @1.7v, rd:  P    P    P    P    P    P    P    P

wrICK @1.7v, rd:  P    P    P    P    P    P    P    P

WR/RD MATRIX AT 400KHz:

5.5v 5.0v 4.5v 3.6v 2.7v 2.5v 1.8v 1.7v

---- ---- ---- ---- ---- ---- ---- ----

wrCHK @5.5v, rd:   P    P    P    P    P    P    F    F

wrICK @5.5v, rd:   P    P    P    P    P    P    F    F

wrCHK @5.0v, rd:   P    P    P    P    P    P    F    F

wrICK @5.0v, rd:   P    P    P    P    P    P    F    F

wrCHK @4.5v, rd:   P    P    P    P    P    P    F    F

wrICK @4.5v, rd:   P    P    P    P    P    P    F    F

wrCHK @3.6v, rd:   P    P    P    P    P    P    F    F

wrICK @3.6v, rd:   P    P    P    P    P    P    F    F

wrCHK @2.7v, rd:   P    P    P    P    P    P    F    F

wrICK @2.7v, rd:   P    P    P    P    P    P    F    F

wrCHK @2.5v, rd:   P    P    P    P    P    P    F    F

wrICK @2.5v, rd:   P    P    P    P    P    P    F    F

wrCHK @1.8v, rd:   F    F    F    F    F    F    F    F

wrICK @1.8v, rd:   P    P    P    P    P    P    F    F

wrCHK @1.7v, rd:   F    F    F    F    F    F    F    F

wrICK @1.7v, rd:   P    P    P    P    P    P    F    F

WR/RD MATRIX AT 1MHz:

5.5v 5.0v 4.5v 3.6v 2.7v 2.5v 1.8v 1.7v

---- ---- ---- ---- ---- ---- ---- ----

wrCHK @5.5v, rd:   P    F    F    F    F    F    F    F

wrICK @5.5v, rd:   P    F    F    F    F    F    F    F

wrCHK @5.0v, rd:   P    F    F    F    F    F    F    F

wrICK @5.0v, rd:   P    F    F    F    F    F    F    F

wrCHK @4.5v, rd:   P    F    F    F    F    F    F    F

wrICK @4.5v, rd:   P    F    F    F    F    F    F    F

wrCHK @3.6v, rd:   P    F    F    F    F    F    F    F

wrICK @3.6v, rd:   P    F    F    F    F    F    F    F

wrCHK @2.7v, rd:   F    F    F    F    F    F    F    F

wrICK @2.7v, rd:   P    F    F    F    F    F    F    F

wrCHK @2.5v, rd:   F    F    F    F    F    F    F    F

wrICK @2.5v, rd:   P    F    F    F    F    F    F    F

wrCHK @1.8v, rd:   F    F    F    F    F    F    F    F

wrICK @1.8v, rd:   P    F    F    F    F    F    F    F

wrCHK @1.7v, rd:   F    F    F    F    F    F    F    F

wrICK @1.7v, rd:   P    F    F    F    F    F    F    F

fSCL@100KHz: Vcc = 01.420  VOLTS

fSCL@200KHz: Vcc = 01.420  VOLTS

fSCL@300KHz: Vcc = 01.460  VOLTS

fSCL@400KHz: Vcc = 01.660  VOLTS

fSCL@500KHz: Vcc = 01.920  VOLTS

fSCL@600KHz: Vcc = 02.160  VOLTS

fSCL@700KHz: Vcc = 02.420  VOLTS

fSCL@800KHz: Vcc = 02.680  VOLTS

fSCL@900KHz: Vcc = 02.960  VOLTS

fSCL@1.0MHz: Vcc = 03.320  VOLTS

fSCL@1.1MHz: Vcc = 04.640  VOLTS

fSCL@1.2MHz: Vcc = 06.000  VOLTS limit!

fSCL@1.3MHz: Vcc = 06.000  VOLTS limit!

fSCL@1.4MHz: Vcc = 06.000  VOLTS limit!

fSCL@1.5MHz: Vcc = 06.000  VOLTS limit!

ICCrd @5.5v, 400KHz =  00.40      MA

ICCrd @5.0v, 400KHz =  00.30      MA

ICCrd @4.5v, 400KHz =  00.25      MA

ICCrd @3.6v, 100KHz =  00.15      MA

ICCrd @2.7v, 100KHz =  00.10      MA

ICCrd @2.5v, 100KHz =  00.10      MA

ICCrd @1.8v, 100KHz =  00.05      MA limit!

ICCwr @5.5v, 100KHz =  03.50      MA

ICCwr @5.0v, 100KHz =  03.20      MA

ICCwr @4.5v, 100KHz =  02.90      MA

ICCwr @3.6v, 100KHz =  02.45      MA

ICCwr @2.7v, 100KHz =  01.50      MA

ICCwr @2.5v, 100KHz =  01.45      MA

ICCwr @1.8v, 100KHz =  00.65      MA

VIL\H @5.5v =  02.000  VOLTS,  02.750  VOLTS

VIL\H @5.0v =  01.850  VOLTS,  02.500  VOLTS

VIL\H @4.5v =  01.700  VOLTS,  02.300  VOLTS

VIL\H @3.6v =  01.400  VOLTS,  01.900  VOLTS

VIL\H @2.7v =  01.100  VOLTS,  01.500  VOLTS

VIL\H @2.5v =  01.000  VOLTS,  01.400  VOLTS

VIL\H @1.8v =  00.600  VOLTS,  01.000  VOLTS

VOL2 @4.5v =  00.040  VOLTS

VOL2 @3.0v =  00.060  VOLTS

VOL1 @1.8v =  00.000  VOLTS

IOL2 @4.5v =  01.01      MA limit!

IOL2 @3.0v =  12.53      MA

IOL1 @1.8v =  03.80      MA

tLOW, no test.

tHIGH (b,a) @5.5v = 0050.00 NS limit!, 0050.00 NS limit!

tHIGH (b,a) @5.0v = 0050.00 NS limit!, 0050.00 NS limit!

tHIGH (b,a) @4.5v = 0051.00 NS limit!, 0051.00 NS limit!

tHIGH (b,a) @3.6v = 0072.00 NS, 0073.00 NS

tHIGH (b,a) @2.7v = 0107.00 NS, 0107.00 NS

tHIGH (b,a) @2.5v = 0120.00 NS, 0120.00 NS

tHIGH (b,a) @1.8v = 0211.00 NS, 0211.00 NS

tI @5.5v = 0040.00 NS

tI @5.0v = 0045.00 NS

tI @4.5v = 0051.00 NS

tI @3.6v = 0069.00 NS

tI @2.7v = 0104.00 NS

tI @2.5v = 0116.00 NS

tI @1.8v = 0203.00 NS

tAA (b,a) @5.5v = 0333.00 NS, 0341.00 NS

tAA (b,a) @5.0v = 0342.00 NS, 0350.00 NS

tAA (b,a) @4.5v = 0353.00 NS, 0362.00 NS

tAA (b,a) @3.6v = 0382.00 NS, 0396.00 NS

tAA (b,a) @2.7v = 0450.00 NS, 0463.00 NS

tAA (b,a) @2.5v = 0480.00 NS, 0488.00 NS

tAA (b,a) @1.8v = 0645.00 NS, 0666.00 NS

tBUF @5.5v = 0053.00 NS

tBUF @5.0v = 0060.00 NS

tBUF @4.5v = 0067.00 NS

tBUF @3.6v = 0091.00 NS

tBUF @2.7v = 0133.00 NS

tBUF @2.5v = 0148.00 NS

tBUF @1.8v = 0254.00 NS

tHD.STA @5.5v = 4500 - 4473.00 NS

tHD.STA @5.0v = 4500 - 4471.00 NS

tHD.STA @4.5v = 4500 - 4470.00 NS

tHD.STA @3.6v = 4500 - 4463.00 NS

tHD.STA @2.7v = 4500 - 4450.00 NS

tHD.STA @2.5v = 4500 - 4444.00 NS

tHD.STA @1.8v = 4500 - 4408.00 NS

tSU.STA @5.5v = 0033.00 NS

tSU.STA @5.0v = 0038.00 NS

tSU.STA @4.5v = 0044.00 NS

tSU.STA @3.6v = 0062.00 NS

tSU.STA @2.7v = 0096.00 NS

tSU.STA @2.5v = 0109.00 NS

tSU.STA @1.8v = 0197.00 NS

tHD.DAT @5.5v = 4739.00 NS - 4750

tHD.DAT @5.0v = 4736.00 NS - 4750

tHD.DAT @4.5v = 4734.00 NS - 4750

tHD.DAT @3.6v = 4726.00 NS - 4750

tHD.DAT @2.7v = 4710.00 NS - 4750

tHD.DAT @2.5v = 4704.00 NS - 4750

tHD.DAT @1.8v = 4668.00 NS - 4750

tSU.DAT @5.5v = 1000 - 0960.00 NS

tSU.DAT @5.0v = 1000 - 0959.00 NS

tSU.DAT @4.5v = 1000 - 0957.00 NS

tSU.DAT @3.6v = 1000 - 0952.00 NS

tSU.DAT @2.7v = 1000 - 0938.00 NS

tSU.DAT @2.5v = 1000 - 0932.00 NS

tSU.DAT @1.8v = 1000 - 0890.00 NS

tSU.STO @5.5v = 1000 - 1029.00 NS

tSU.STO @5.0v = 1000 - 1031.00 NS

tSU.STO @4.5v = 1000 - 1034.00 NS

tSU.STO @3.6v = 1000 - 1042.00 NS

tSU.STO @2.7v = 1000 - 1059.00 NS

tSU.STO @2.5v = 1000 - 1065.00 NS

tSU.STO @1.8v = 1000 - 1108.00 NS

tDH = tAA.

tWR @5.5v =  01.20mS

tWR @5.0v =  01.20mS

tWR @4.5v =  01.20mS

tWR @3.6v =  01.35mS

tWR @2.7v =  01.35mS

tWR @2.5v =  01.35mS

tWR @1.8v =  01.50mS

----------------------------------------